SPECIFICATION

Work reference GWR363

The British High Commission Yaounde has a requirement for remediation works on perimeter walls in three of its properties (CMY049C, CMY046C & CMY002A) in the Bastos area. For schedule of works, refer to Schedule 1, Schedule 2 and Schedule 3 accordingly.

All the work shall be in accordance with recognized UK and International Building and Construction codes. Construction shall abide by all the Foreign Development and Commonwealth Office (FCDO) rules and regulations including security and safety regulations.

All work described in this Scope of Work shall be completed by the contractor. The contractor shall provide qualified supervisory, technical and labour personnel capable of meeting the requirements. The labour force shall possess the constructional, carpentry, masonry and painting skills for this project and sufficient staff to accomplish the work in a timely manner. The contractor shall provide all necessary material, tools, equipment, vehicles required for this work. Contractor should ensure the minimum disturbance and no damages to the existing property of the premises.

Scope of Works

  1. GWR363 CMY049C (schedule 1)

WEST, NORTH & EAST WALLS

The affected wall lengths are circa

West wall 35m

Collapsed and rebuilt section of north wall 35m

North wall 45m

East wall 30m

Prop the west, north and east walls and bring down all the elevated sections similar shown in Figure 27 and Figure 28 to the original height. (see appendix)

Strip off the existing render from the Compound side to expose the blockwork and RC wind posts.

Dig the soil on the Compound side along the walls down to the wall base.

Apply fabric reinforcement mesh to the wall surface from the Compound side with staggered anchors. For details, refer to Figure 36 in the Appendix.

Install RC strip foundations and underpin the wall at regular intervals of 1.5m. For details, refer to Figure 36 in the Appendix.
Render the meshed wall surface with a minimum of 40mm thick shotcrete. For details, refer to Figure 36 in the Appendix.

Install cranked metal fencing and barbed wire. For details, refer to Figure 29 in the Appendix.

GWR365 CMY046C (schedule 2)

RETAINING (WEST) WALL

The affected wall length is circa 25m and the average height is 4.5m shown in Figure 12.

Remove the water tank and canopy shown in Figure 26 to allow access to the wall.

Prop the wall from the Compound side. Strip off any existing render.

Apply fabric reinforcement mesh to the wall surface tying it to the wall with staggered anchors. For details, refer to Figure 36 in the Appendix.

Install RC pad foundations and buttresses. For details, refer to Figure 34, Figure 35 and Figure 37 in the Appendix.

Install weep holes.

Render the meshed wall surface with a minimum of 40mm thick shotcrete. For details, refer to Figure 36 in the Appendix.

Install staggered tieback self-drilling soil anchors and inject a grout. Spacing of soil anchors to be 1.5 - 2.0m. For details, refer to Figure 30, Figure 31 and Figure 32 in the Appendix.

GWR366 CMY002A (schedule 3)

NORTH WALL

The affected wall length is circa 50m shown in Figure 11.

Prop the wall from both sides.

Strip off the existing render from the Compound side to expose the blockwork and RC wind posts.

Dig the soil on the Compound side along the wall down to the wall base.

Apply fabric reinforcement mesh to the wall surface from the Compound side with staggered anchors. For details, refer to Figure 36 in the Appendix.

Install RC strip foundations and underpin the wall at regular intervals of 1.5m. For details, refer to Figure 36 in the Appendix.

Render the meshed wall surface with a minimum of 40mm thick shotcrete. For details, refer to Figure 36 in the Appendix.

Install cranked metal fencing and barbed wire. For details, refer to Figure 29 in the Appendix.

2. Specification

2.1. Works to be completed to the following standards:

Local Building Regulations

BS EN 1990 Basis of structural design BS EN 1991 Actions on structures

BS EN 1992 Design of concrete structures BS EN 1993 Design of steel structures
BS EN 1996 Design of masonry structures

2.2. Contractor Requirements

The Contractor shall

Provide written Risk Assessments and Method Statements specific to proposed works with particular emphasis on risks associated with working at height and public who might be reasonably impacted by the works.

Allow for and provide all the necessary work and safety equipment to undertake the works including all access equipment.

Make safe any areas where features have been removed if they pose a health and safety hazard.

Remove and dispose off-site all identified waste materials in accordance with local authority guidance and best practice.

Make good damage arising from demolition and construction works.

Give notice and inform the PM about defects exposed or becoming apparent. Design and provide any temporary works as required.

The Contractor shall provide the following supporting information

Proposals for the organisation and execution of the works.

Commencement and completion dates and relationship between various activities. Listings of manpower, materials and plant requirements.

Emergency Procedures.

Method for removal, transportation, and disposal of construction waste.

Identification and location of services above and below ground that may be impacted by the works.

2.3. Masonry

Masonry shall be in accordance with BS EN 1996.

Workmanship to comply with the clauses in BS EN 1996 and PD 6697.

Cutting, dressing, laying and jointing of masonry to be carried out by masons skilled in the work required.

Provide temporary support to structure. Maintain and modify support as required during masonry repair work.

Ensure that structural stability of the wall and of all temporary work is maintained throughout.

Before delivery to site, inspect and check masonry units to match existing and comply with specifications.

When repairing masonry, remove soft mortar by brushing, vacuuming or raking with chisel in preference to cutting with hammer and chisel.

When repairing masonry, cut out defective / damaged masonry units until structurally sound material is reached.

When laying new masonry, keep it clean during construction.

Dampen masonry, wet existing masonry, and lay bricks on a full even bed of mortar with all joints filled.

2.4. Concrete

Concrete shall be in accordance with BS EN 1992 and BS 8500.

Provide concrete producer with information required by BS 8500-1.

Materials and workmanship are to comply generally with BS EN 1992-1-1 and BS EN 13670.

All reinforced concrete not in contact with the ground to be designated concrete C28/35 to BS 8500 and BS EN 206-1 with CEM1 OPC to BS EN 197 and 20mm max aggregate. All reinforced concrete in contact with the ground such as foundations or retaining walls to be constructed in designated concrete C28/35 using sulphate resistant cement and 20mm max aggregate to BS 8500 and BS EN 206-1.

Ready mixed concrete must be obtained from a plant, which holds a current Certificate of Accreditation under the Quality Scheme from a local approved body.

Site-mixed concrete may be used when agreed with an Engineer. An agreed prebatched and bagged proprietary concrete must be used unless an alternative site batched concrete has been agreed with an Engineer.

When the ambient air temperature is over 30°C additional curing measures to be applied.

Concrete cubes to be tested for compressive strength for all reinforced concrete elements. 3 samples per pour or per 50m3. One 7-day test, one 28-day test and one sample for future testing if required. All tests to be carried out by UKAS

accredited laboratory or equivalent. Testing to BS EN 206-1, annex B and BS 8500-1, annex B. Results are to be submitted to the Engineer within 5 working days of the test.

2.5. Reinforcement

All reinforcement shall comply with the requirements of BS 4449, BS 4483, and BS 8666 as appropriate.

Reinforcement in accordance with BS 4449 shall be deformed with ribbed surface and have characteristic yield strength of 500 N/mm2 unless noted otherwise.

All tying of reinforcement shall be carried out with black annealed mild steel 16 gauge tying wire, unless noted otherwise.

Minimum embedment and lap lengths for all reinforcement in proposed structure shall be in accordance with the recommendations of BS EN 1992.

Links shall be bent 135°.

Welding of reinforcement shall not be permitted. Site bending
  - The curvature should be as constant as practicable

  - Bending should be in one operation at a constant rate

  - Reinforcement should not be warmed above 100 °C

  - The bend radius shall not be less than that given in BS 8666 and Cl. 6.3(2) of BS EN 13670: 2009

3. PROJECT SCHEDULE & WORKERS.

Schedule 1-3 in appendix are high-level estimate for these works. Programme duration and milestones to be provided by contractor as part of quote based on the scope of works.

Close attention should be given to the following:

Site inspection is required prior to when work will commence

Work days to be coordinated with FCDO Clerks of Works, BHC Estate Officer/Manager, and Contractor to submit a full programme of works prior to works commencing

Work hours will be from 0900 to 1530hrs Monday to Thursday and Friday 0900-1330hrs. weekend might be inclusive (note that this is subject to change)

Job completion certificate to be signed by both contractor and foreman after completion of all works.

Site supervisor will ensure that all equipment used during the project is in safe operating condition. All personnel on the job site will be given the appropriate safety equipment. The British High Commission reserves the right to stop the work if any unsafe conditions are found.

Risk assessment and method statement is to be submitted alongside the quotation Risk assessment, method statement and register to be on site for the duration the
work is been carried out at all times.

All electrical equipment such as drills, grinding, buffing machines and any extension cords must be properly grounded and be free from any defect in the insulation

All required mandatory document (Working in confined spaces, Working at Height, Hot Works permits) are signed before commencement of work.

All work tools to be in good condition and used in a proper manner.

APPENDIX

CMY049C

Figure 38: Indicative Site Plan and Walls

Schedule 1

Schedule 2

Schedule 3